## Slide 1: Charged particle detection with superconducting nanowire single photon detectors (SNSPDs)

## Slide 2: Potential use case in FCC
Interaction Points
RF System
Beam Axis
1 – 3 m
1 – 3 m
FCC Lepton detector (CLD) based on CLICdet
Luminometers
FCC e+e-
~100 km double ring collider
2 IPs with 30 mrad crossing angle
angle 91 GeV (Z) – 365 GeV (ttbar)
Luminosity: up to 500×1034 cm-2s-1
SNSPD based Luminometer
Sub-per mill resolution through small angle Bhabha scattering
Goal of 10-4 precision on absolute luminosity
Readout at Bunch-crossing rates with < 20ns shaping time
Notes: What are the research questions, state of the art, intended contributions to the state-of-the-art?
What are the contributions of this project to the overall questions of the NCCR?
Establish the magnitude of the problem/question and who is working on it

## Slide 3
Superconducting nanowire detectors
Initially developed for photon counting, but can be used for direct particle detection or coupled to scintillators

## Slide 4: Instrument setup
SNSPD
Electric diagram:
Current source: Yokogawa GS200
Voltage source up to 32V
Current source up to 200mA
5 μA accuracy
Bias Tee: ZX85-12G-S+
Max voltage: 25V
Max current: 400mA
RF Power: 30dBm
Bandwidth: 12GHz
Amplifier: ZX60-3018G-S+
Bandwidth: 3GHz
Output power: 12.8dBm
Max current: 45mA
Max voltage: 12.5V
Oscilloscope: Tektronix DPO7354
Bandwidth: 3.5GHz
40GS/s
4 channels
FastAcq: 250 000 triggers/s
Current source
Bias tee
Amplifier
Amplifier
Oscilloscope
RF
RF + DC
DC

## Slide 5: Liquid Helium cryostat
LHe cryostat:
Cooldown time: ~4h
Lowest temperature: 4.2K
Experiment time: ~8h
Advantages:
Rapid cooldown and setup
Disadvantages:
2 readout channels
Requires cooling every 24h
Window
Chip holder

## Slide 6: Closed cycle cryostat
Closed cycle cryostat:
Cooldown time: ~8h
Lowest temperature: 2.28K
Experiment time: infinite
Advantages:
16 readout channels
No daily maintenance
Disadvantages:
Extensive setup time
Window
Chip holder
Readout
Cold stage

## Slide 7: Goals of the thesis
SNSPD characterization of NbTiN, NbN and
Designing, building and setting up a radioactive experiment
SNSPD characterization using electrons

## Slide 8: SNSPD characterization experiment

## Slide 9
IV measurement
Critical current
Hysteresis current
Example of an IV measurement

## Slide 10
Trigger level measurement
Trigger level curve example
1
2
3

## Slide 11
Photon and dark count rates
Photon count rate (PCR) example
Dark count rate (DCR) example
Dark counts with no laser source
Photon count with a laser source

## Slide 12: Optical characterization results

## Slide 13
NbTiN SNSPD (A)
IV curve
Trigger level
PCR
DCR

## Slide 14
NbTiN SNSPD (B)
PCR vs DCR comparison
IV curve

## Slide 15
Deposition method
Magnetron sputtering
HPCVD
Tc ~ 35K
Tc ~ 17K

## Slide 16
SNSPD
Critical current vs wire width
Hysteresis current vs wire width
IV curve
Critical current vs temperature

## Slide 17
NbN SNSPD
IV curve
Trigger level
PCR
DCR

## Slide 18: Radioactive experiment

## Slide 19
Experimental setup
Cryostat
Cryostat piece
Cryostat piece
Lead castles

## Slide 20
Strontium90 source
28 MBq source (originally 37MBq)
550 KeV decay energy (Strontium 90)
Into 2.3 MeV decay energy (Yttrium 90)
Bought: 26/03/2012
Serial number: VZ-3721-001
Strontium90 decay chain
Strontium90 beta spectrum
Radioactive source model
Collimator model

## Slide 21: Collimator design
Radioactive
source
Collimator
SNSPD
128.8mm
y
x
2.5+0.5x mm
Minimum plexiglass thickness: 1.6cm
Length of collimator: 4cm
Collimator opening: 0.67mm
Collimator model
Ray casting diagram
Collimator length as a function of collimator radius

## Slide 22: Holder design
Collimator holder
LGAD holder

## Slide 23
Cryostat window issues
As we can see, bremsstrahlung cross section increases with Z.
The current window installed on the cryostat is a 2.5mm thick, aluminium window, which will create bremsstrahlung radiation and thus unwanted dark rates, making it unusable.
Cryostat window requirements:
Low Z material
Small beta spectrum attenuation
Opaque (optional)
Low cost
Vacuum resistant

## Slide 24
Cryostat window minimum thickness
Minimum window thickness equation:
K : 0.75 (empirical factor accounting for the clamping method)
D : Diameter
P : Pressure difference
: Rupture modulus
Sf : Safety factor taken as 4
T : Window thickness
: Maximum force
Material | Aluminium Nitrite | Aluminium Oxide | Aluminium | Plexiglass | Silicon
Density () | 3.255 | 3.98 | 2.7 | 1.18 | 2.38
Rupture Modulus (MPa) | 367 | 800 | 280 | 72 | 200
Minimum Thickness (mm) | 0.26 | 0.3 | 0.18 | 0.58 | 0.35
Material | Aluminium Nitrite | Aluminium Oxide | Aluminium | Plexiglass | Silicon
 | 3.255 | 3.98 | 2.7 | 1.18 | 2.38
Rupture Modulus (MPa) | 367 | 800 | 280 | 72 | 200
Minimum Thickness (mm) | 0.26 | 0.3 | 0.18 | 0.58 | 0.35

## Slide 25
Stopping power analysis
The data was taken from the NIST ESTAR database

## Slide 26
Beta Spectrum analysis
Beta Spectrum formula:
K : Kinetic energy
Q : Total energy
m : Electron mass
c : speed of light
E : Total electron energy
A,B : Constants specific to the radioactive source
F(Z, K) : Fermi correction to the spectrum
The energy lost by electrons in MeV/cm was calculated as the product of the stopping power and the material density
Because the beta spectrum is very similar among the five materials, we have decided to make the cryostat windows out of Plexiglass !
Window model

## Slide 27: Radioactive experiment results

## Slide 28
NbTiN SNSPD (A)
Window and foil:
Prevents ~90% of dark counts
Stops the low energy electrons
Creates x-rays through Bremsstrahlung
Only foil:
More dark counts
Better Beta spectrum
Small number of x-rays created
Comparison between having the source present or not

## Slide 29
NbTiN SNSPD (A)
Median background rate: 7/s
Median radioactive rate: 6/s
Poisson fit of recorded counts per 3s
Recorded counts for varying duration

## Slide 30
NbN SNSPD
Normalized counts as a function of bias current

## Slide 31
NbTiN SNSPD (B)
Median particle rate: 1.03/s
Poisson fit of recorded counts per 3s
Counts as a function of duration

## Slide 32
NbTiN SNSPD (B)
The signal !
τ
τ = 196ns

## Slide 33
Conclusion
NbTiN, NbN and SNSPDs have been characterized
Radioactive experiment was designed, built and setup
Electron detection using NbTiN and NbN SNSPDs
First NbTiN SNSPD electron signal obtained

## Slide 34
Thank you !
Any questions ?

## Slide 35
Photon count correction
Due to the dead time inherent to SNSPDs and the instruments used, a correction to the counts might be necessary. The SNSPD is considered to be paralyzable (20ns), and the photon counter was approximated to a non paralyzable instrument with 5ns dead time.
Paralyzable dead time correction:
Non-paralyzable dead time correction:
Dead time correction comparison