## Slide 1: The new wafer design
Alexandre Hennessy, Vagelis Gkougkousis
03/02/2026

## Slide 2: Improved wafer layout:
Layout information:
160 unique SNSPDs
47 SNSPD die and 18 test structures
7 duplicates with variable relative positions
50μm dicing lines
50μm marker width
Key differences:
Bigger chips with 8 SNSPDs instead of 1
Less photolithography required
Silicon wafer:
Monocrystalline Fz Si
<100> or <111> orientation
4” diameter
525μm thickness
Double sided polish
P-type boron doping
10KOhm.cm
1
A. Hennessy, E. L. Gkougkousis
03/02/2026

## Slide 3: Masks:
Dicing lines etching, 2μm deep and 100nm wide
Alignment markers, 20μm marks
Chip gold marker, 100nm wide, photolithography
Gold pads and SNSPD identifier
Wide e-beam lithography (100nm)
Narrow e-beam lithography (SNSPDs, 30nm)
2
A. Hennessy, E. L. Gkougkousis
03/02/2026

## Slide 4: SNSPD characteristics:
Pixel size | Width | Fill factor
100 | 100 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 200 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 500 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 1000 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
Pixel size | Width | Fill factor
200 | 100 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 200 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 500 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 1000 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
Pixel size | Width | Fill factor
300 | 100 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 200 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 500 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 1000 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
Pixel size | Width | Fill factor
1000 | 100 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 200 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 500 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
 | 1000 | 30%
 |  | 40%
 |  | 50%
 |  | 60%
Total: 160 unique SNSPDs
3
A. Hennessy, E. L. Gkougkousis
03/02/2026

## Slide 5: Die geometry:
450μm
250μm
550μm
200μm
700μm
50μm
700μm
700μm
550μm
550μm
550μm
450μm
450μm
Second SNSPD layout for pixels <500μm
250μm
4
A. Hennessy, E. L. Gkougkousis
03/02/2026
7.05mm
4.05mm

## Slide 6: Test structures (1):
Inductance measurements with single wires:
100nm wire width
Same length as other SNSPDs on the wafer
Accurate comparison between SNSPD and wire inductance
Length varies from 3 to 60mm
is the wire length
is the pixel size
is the filling factor
is the wire width
Film uniformity measurements:
4x4mm die
Measurement of:
  Residual resistivity ratio
  RT(B), including ΔT
  London penetration depth
  Coherence length
  Diffusion coefficient
4mm
4mm
5
A. Hennessy, E. L. Gkougkousis
03/02/2026

## Slide 7
Test structures (2):
Proximity effect of wires:
Electrical characterization for 1 to 3 wires with varying wire distances (corresponding to the SNSPD Fill factors on the wafer)
Standard litho resolution test:
Verify the capabilities of lithography, including:
  Meander proximity effect
  Beam resolution
  Scribing speed and error rate
  Overhang or underhang creation
100nm
100nm
100nm
100nm
100nm
6
A. Hennessy, E. L. Gkougkousis
03/02/2026

## Slide 8
Test structures (3):
7
A. Hennessy, E. L. Gkougkousis
03/02/2026
Proximity effect of wires:
Electrical characterization for 2 and 3 wires with varying wire distances (corresponding to the SNSPD Fill factors on the wafer) and isolated contact pads
3-Wire measurement
2-Wire measurement

## Slide 9: Time/Cost analysis:
Time difference:
Time and cost wise, the bulk of the time is taken by the setup of each machine (billable by the hour)
Metric: | Fully used wafer (~1000SNSPDs) | Only 16 SNSPDs
Time difference: | 45 h | 33 h
Cost difference: | 3780 CHF | 3000 CHF
Wafer: | One wafer per production | One wafer for several productions
Main changes:
SPTS rapier photolithography:
  4 extra hours → 200 CHF required
RAITH e-beam lithography:
  4 extra hours → 200 CHF required
Heidelberg photolithography:
  4 extra hours → 130 CHF required
8
A. Hennessy, E. L. Gkougkousis
03/02/2026

## Slide 10: Conventional SNSPD fabrication:
Next steps: After fabrication, the wafer can be dice into single SNSPD die. SEM/AFM pictures of each sample and, for the future, the samples can be bonded at CMi.
Step 1: Creation of the dicing lines
Step 2: Thin film deposition (NbN, NbTiN) using magnetron sputtering
Step 3: SNSPD patterning though 2 steps of e-Beam lithography (Coarse + Fine)
Step 4: Gold deposition through evaporation on lift-off resist
Step 5: Lift-off and cleaning
9
A. Hennessy, E. L. Gkougkousis
03/02/2026